Informal document No. 6

(54th GRRF, 6-8 October 2003,

agenda item 3.)

## PROPOSAL FOR DRAFT AMENDMENTS TO REGULATION No. 90

(Replacement brake linings)

Transmitted by the expert of the Federation of

European Manufacturers of Friction Materials (FEMFM)

Note:  The text reproduced below was prepared by the expert from FEMFM in order to strengthen some prescriptions of the Regulation. It completes the proposals appearing in document TRANS/WP.29/GRRF/2001/18.

A.	PROPOSAL

Annex 3,

Paragraph 2.1.2.1., amend to read:

"2.1.2.1....make three brake applications with the initial speed (vI) and final speed (vF) as given in the table below:

| Axle | Braking Interval | Evaluation Window | Remark |
| --- | --- | --- | --- |
|  | vI | vF | v1 | v2 |  |
| Front | 70 110 145 | 25 45 55 | 60 100 135 | 30 50 65 | if vmax > 150 |
| Rear | 50 70 100 | 20 25 40 | 40 60 90 | 25 30 45 | if vmax > 150 |

All speeds in km/h

Calculate the mean fully development deceleration for the corresponding evaluation window between the speeds v1 and v2 in the table above."

Paragraph 2.2.4.1., amend to read:

"2.2.4.1.,... make three brake applications with the initial rotational speed (vI) and final rotation speed (vF) corresponding to the vehicle linear speed as given in the table below:

| Vehicle Category | Axle | Braking Interval | Evaluation Window | Remark |
| --- | --- | --- | --- | --- |
|  |  | vI | vF | v1 | v2 |  |
| M1 | front | 80 125 165 | 30 50 60 | 70 115 150 | 35 60 65 | if vmax > 150 |
| M1 | rear | 85 125 165 | 30 50 40 | 75 115 150 | 35 60 65 | if vmax > 150 |
| M2 | front | 85 130 165 | 35 50 35 | 75 120 150 | 40 60 45 | if vmax > 150 |
| M2 | rear | 75 110 150 | 30 50 60 | 70 100 135 | 40 55 65 | if vmax > 150 |
| N1 | front | 85 130 165 | 30 45 25 | 75 120 150 | 35 55 35 | if vmax > 150 |
| N1 | rear | 80 115 160 | 35 45 65 | 70 105 145 | 40 50 75 | if vmax > 150 |

All speeds in km/h

Calculate the mean fully development deceleration for the corresponding evaluation window between the speeds v1 and v2 in the table above."

Annex 4,

Paragraph 1.2.2.2.1., amend to read:

"1.2.2.2.1....make three brake applications with the initial speed (vI) and final speed (vF) as given in the table below:

| Braking Interval | Evaluation Window | Remark |
| --- | --- | --- |
| vI | vF | v1 | v2 |  |
| 40 60 80 | 20 35 55 | 35 55 75 | 25 40 60 | if vmax > 90 |

All speeds in km/h

Calculate the mean fully development deceleration for the corresponding evaluation window between the speeds v1 and v2 in the table above."

Paragraph 2.2.3.1., amend to read

"2.2.3.1....make three brake applications with the initial rotational speed and final rotational speed corresponding to the vehicle linear speeds vI and vF as given in the table below:

| Braking Interval | Evaluation Window | Remark |
| --- | --- | --- |
| vI | vF | v1 | v2 |  |
| 55 80 110 | 30 45 75 | 50 75 105 | 35 50 80 | if vmax > 90 |

All speeds in km/h

Calculate the mean fully development deceleration for the corresponding evaluation window between the given speeds v1 and v2 in the table above."

*     *     *

B.	JUSTIFICATION

Document GFFR/2001/18 has explained in detail the reasons for the proposal to introduce "snub braking" instead of stop braking for the evaluation of the speed sensitivity. It has also pointed out that vehicle test and dynamometer test does not always correspond well regarding the absorbed energy. This means speed sensitivity test on the vehicle and dyno test are at present not fully comparable.

The proposals in GRRF/2001/18 tried to overcome these problems. However, during the discussion in the 50. GRRF some delegates felt that the proposal seemed to weaken existing requirements whereas the principle of snub braking was not argued.

A small adhoc working group came together in February 2002 and discussed the issues raised in GRRF. The proposal above is the result out of this discussion.

The main amendments to GRRF 2001/18 are the definition of the braking interval and the evaluation window. The braking interval is calculated such that the energy absorbed is equal to the existing requirements in Regulation 90, which is proven in the table below where the factor C shows the relation of the braking energies (C>1 means the braking energy in the stop braking is greater than in the snub braking). The evaluation window guarantees a repeatable and precise.

| Axle | vI | vF | vStop | C |
| --- | --- | --- | --- | --- |
| front | 70 | 25 | 65 | 0,99 |
| front | 110 | 45 | 100 | 0,99 |
| front | 145 | 55 | 135 | 1,01 |
| rear | 50 | 22 | 45 | 0,96 |
| rear | 70 | 25 | 65 | 0,99 |
| rear | 100 | 40 | 90 | 0,96 |

In the table below the factor F as defined in GRRF 2001/18 is calculated for all test conditions for speed sensitivity in annex 3 and 4. The values are all close to 1 proving that vehicle test and dyno test are comparable for the new requirements.

| Vehicle Category | Axle | Vehicle Test | Dyno Test | ma/M | F |
| --- | --- | --- | --- | --- | --- |
|  |  | Brake Application | Brake Application |  |  |
|  |  | vI | VF | VI | VF |  |  |
| M1 | front | 70 | 25 | 80 | 30 | 0,77 | 1,009 |
| M1 | front | 110 | 45 | 125 | 50 | 0,77 | 0,997 |
| M1 | front | 145 | 55 | 165 | 60 | 0,77 | 0,989 |
| M1 | rear | 50 | 20 | 85 | 30 | 0,32 | 1,038 |
| M1 | rear | 70 | 25 | 125 | 50 | 0,32 | 1,018 |
| M1 | rear | 100 | 40 | 165 | 40 | 0,32 | 1,024 |
| M2 | front | 70 | 25 | 85 | 35 | 0,69 | 1,033 |
| M2 | front | 110 | 45 | 130 | 50 | 0,69 | 1,014 |
| M2 | front | 145 | 55 | 165 | 35 | 0,69 | 1,003 |
| M2 | rear | 50 | 20 | 75 | 30 | 0,44 | 1,010 |
| M2 | rear | 70 | 25 | 110 | 50 | 0,44 | 1,012 |
| M2 | rear | 100 | 40 | 150 | 60 | 0,44 | 1,010 |
| N1 | front | 70 | 25 | 85 | 30 | 0,66 | 1,024 |
| N1 | front | 110 | 45 | 130 | 45 | 0,66 | 1,026 |
| N1 | front | 145 | 55 | 165 | 25 | 0,66 | 1,025 |
| N1 | rear | 50 | 20 | 80 | 35 | 0,39 | 1,041 |
| N1 | rear | 70 | 25 | 115 | 45 | 0,39 | 0,979 |
| N1 | rear | 100 | 40 | 160 | 65 | 0,39 | 1,008 |
| M3,N2,N3 | f+r | 40 | 20 | 55 | 30 | 0,55 | 1,027 |
| M3,N2,N3 | f+r | 60 | 35 | 80 | 45 | 0,55 | 0,987 |
| M3,N2,N3 | f+r | 80 | 55 | 110 | 75 | 0,55 | 0,948 |

A vehicle test has been carried out in order to compare the existing with the new requirement using three different materials (Material A is the OE material). In the graphs below the bars show the performance achieved comparing stop and snub braking. The dots linked with a straight line show the maximum disk temperature achieved in the tests. Regarding the speed sensitivity of the three materials both stop and snub braking come to a similar result. The temperatures show that in this case the snub braking is a little more severe, however, the difference is very small.