CLEPA's comments on ECE/TRANS/WP.29/GRE/2006/39

Note:	The text reproduced below was prepared by the experts from CLEPA in order to propose amendments to ECE/TRANS/WP29/GRE/2006/39, tabled by India.  The modifications to ECE/TRANS/WP29/GRE/2006/39 are marked in bold and/or strikethrough characters.

A.	PROPOSAL

Paragraph 7.2.1., amend to read:

"7.2.1.	When subjected to a continuous spraying action for 60 seconds on the test component in its normal mounting conditions, a test sample shall show no damage to the retro-reflective surface or delaminate from the substrate or separation from the sample mounting surface under the following set-up parameters:

(a)	Water/wash solution pressure 8 ± 0.2 MPa;

(b)	Water/wash solution temperature 60° - 5 °C;

(c)	Water/wash solution flow rate 6 to 7 l/min;

(c)	The tip of the cleaning wand to be positioned at distance of 600 ± 20 mm away from the retro-reflective surface;

(d)	Cleaning wand to be held at no greater angle than 45 degrees from perpendicular to the retro-reflective surface;

(e)	40 degree nozzle creating wide fan pattern."

B.	JUSTIFICATION

This proposal is in a line with the proposal by CLEPA for amendments to Regulation No. 104 (ECE/TRANS/WP.29/2006/66 and ECE/TRANS/WP.29/2006/66/Amend.1), adopted by WP.29 and AC.1 at their June 2006 sessions (see report ECE/TRANS/WP.29/1052, paras. 53 and 80).

- - - - -