## Slide 1: ETRTO study on the Dimensional Requirements for tyres with radial or run flat structure after having performed the load speed endurance test
European Tyre and Rim Technical Organisation
Informal document GRBP-71-07
Agenda item 5 (a)
GRBP session 71, January 2020

## Slide 2
European Tyre and Rim Technical Organisation 1
Outline
Background
ETRTO study
Results
Amendment proposal
Implementation proposal

## Slide 3
European Tyre and Rim Technical Organisation 2
1. Background
The existing UN Regulations No 30, 54 and 75 have provisions
with dimensional requirements for tyres with all types of structure after having performed the load/speed performance test:
§6.2.3 in R30, R54 and R75 requires:
The outer diameter of the tyre, measured six hours after the load/speed performance test, must not differ by more than ±3.5 per cent from the outer diameter as measured before the test.
In context of the Amendment 2 to the Tyre GTR, based on Tyre Industry experience, the proposal was made by the Tyre Industry and the IWG Tyre GTR to remove those dimensional requirements for tyres with radial and run flat structures, and Contracting Parties requested data and evidence before agreeing with the proposal.

## Slide 4
European Tyre and Rim Technical Organisation 3
2. ETRTO study
The aim of ETRTO study is to provide evidence that the dimensional requirements for tyres with radial or run flat structure after having performed the load/speed performance test are not relevant.
The study is also extended to all tyres falling under load/speed test following UN Reg.54 [and to all tyres covered by UN Reg.75].

## Slide 5
European Tyre and Rim Technical Organisation 3
2. ETRTO study
Number of companies: 5 (Europe and Japan)
Tyre classes: Passenger car, Commercial vehicle and motorcycle
Number of tyres tested:
C1: 86 radial + 53 run flat
C2: 51 radial
C3: 33 radial
Motorcycle: study on going

## Slide 6
European Tyre and Rim Technical Organisation 4
3. Results
For C1, C2 and C3 tyres, the Outer Diameter of each tyre was measured before and just after the test.
All details are in the appendix of this presentation
C1 Radial |  |  | 
number of tyres | average diameter increase | minimum | maximum
86 | 0,39% | -0,08% | 1,15%
C2 Radial |  |  | 
number of tyres | average diameter increase | minimum | maximum
51 | 0,26% | -0,39% | 0,78%
C3 Radial |  |  | 
number of tyres | average diameter increase | minimum | maximum
33 | 0,34% | 0,07% | 0,79%
C1 (Run flat) |  |  | 
number of tyres | average diameter increase | minimum | maximum
53 | 0,51% | 0,00% | 1,31%

## Slide 7
European Tyre and Rim Technical Organisation 5
4. Amendment proposal
Based on the study results, it is proposed to amend the UN Regulations No 30, 54 [and 75] by removing the requirements for tyres with radial and run flat structure in paragraph 6.2.3. as the tolerance for the outer diameter growth of maximum 3,5% is very far from being reached.
Proposal for UN Reg.30
“For diagonal (bias-ply) tyres or bias belted tyres, the outer diameter of the tyre, measured six hours after the load/speed performance test as specified in paragraph 2. of Annex 7, must not differ by more than +/- 3.5 per cent from the outer diameter as measured before the test.”
Proposal for UN Reg.54
“For diagonal (bias-ply) tyres, the outer diameter of the tyre, measured six hours after the load/speed endurance test, must not differ by more than +/- 3.5 per cent from the outer diameter as measured before the test.”

## Slide 8
European Tyre and Rim Technical Organisation 6
5. Implementation proposal
ETRTO proposes to GRBP to amend the UN Regulations No 30, 54 according to the example shown in the proposal of previous slide, when a future amendment proposal to that Regulation will be submitted to GRBP.
The justification will then refer to this informal document for UN Reg.30 and 54.
Regarding UN Reg.75, when the study is completed, an additional informal document will be presented to GRBP to support the proposal of amendment.

## Slide 9
European Tyre and Rim Technical Organisation
Appendix

## Slide 10
Appendix

## Slide 11
Appendix

## Slide 12
Appendix

## Slide 13
Appendix

## Slide 14
Appendix

## Slide 15
Appendix

## Slide 16
Appendix